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HANGZOU ZHENYAN CHEMICAL CO., LTD.
No.404-3 Bonded Building, Airport Economic Area, Hangzhou, China
Tel: +86-13454156527    https://www.zhenyanchem.com/
[bookmark: Applications：][bookmark: Package：________________________________][bookmark: *Product_specific_and_application_inform]Color Type	     Monoazo Lake
Color Index No.	P.R.57:1 CAS NO.	5281-04-9
Structure:

[image: ]Description：
· [bookmark: OLE_LINK1]There are many different color shades from yellowish to bluish products for offset inks.
· W5713 is semi-transparent high gloss for water-based ink.
· S5714 is bluish 4BGL for Solvent-based ink with low viscosity and high gloss.
· S5715 is yellowish for Solvent-based ink.
· P5711 Rubine 4BP is superfine grinding for plastic and powder coating.
Physical properties and Fastness：
	[bookmark: _Hlk187069756]Density (g/cm3)
	1.65-2.11

	Oil absorption (ml/100g)
	45±5

	Water soluble matter (%)
	≤2.5

	PH Value
	6.5-8.0

	Heat Resistance (°C)
	160~220°C

	Light Fastness
	5

	Water Resistance
	4

	Oil Resistance
	4

	Acid Resistance
	4

	Alkali Resistance
	4~5

	Alcohol Resistance
	4

	Migration
	4



Color card:
[image: ]
Applications：

	
Inks
	Offset Ink
	●

	
	Water Based Ink
	●

	
	Solvent Based Ink
	●

	Plastic
	PVC/LDPE
	●

	Paint
	Decorative Paint
	○

	
	Powder Coating
	●


[bookmark: OLE_LINK8]Remark: ●High Recommendation;
[bookmark: OLE_LINK2]○Recommendation; -Limit Suitability
[bookmark: Storage_conditions：]Storage conditions：
[bookmark: Should_be_sealed_for_avoiding_light_and_]Should be sealed for avoiding light and moisture.

Package：
25kgs craft bag with Carton box on pallet.



Please note: ***This technical index and recommending application information is based on the present knowledge for reference only. Necessary test is needed before you put into use. ***
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