Lithol Rubine (Calcium)

Color Type	     Monoazo Lake

Color Index No.	P.R.57:1 CAS NO.	5281-04-9

Structure:

Description：

- There are many different color shades from yellowish to bluish products for offset inks.

- W5713 is semi-transparent high gloss for water-based ink.

- S5714 is bluish 4BGL for Solvent-based ink with low viscosity and high gloss.

- S5715 is yellowish for Solvent-based ink.

- P5711 Rubine 4BP is superfine grinding for plastic and powder coating.

Physical properties and Fastness：

| Density (g/cm3) | 1.65-2.11 |
| --- | --- |
| Oil absorption (ml/100g) | 45±5 |
| Water soluble matter (%) | ≤2.5 |
| PH Value | 6.5-8.0 |
| Heat Resistance (°C) | 160~220°C |
| Light Fastness | 5 |
| Water Resistance | 4 |
| Oil Resistance | 4 |
| Acid Resistance | 4 |
| Alkali Resistance | 4~5 |
| Alcohol Resistance | 4 |
| Migration | 4 |

Color card:

Applications：

| Inks | Offset Ink | ● |
| --- | --- | --- |
|  | Water Based Ink | ● |
|  | Solvent Based Ink | ● |
| Plastic | PVC/LDPE | ● |
| Paint | Decorative Paint | ○ |
|  | Powder Coating | ● |

Remark: ●High Recommendation;

○Recommendation; -Limit Suitability

Storage conditions：

Should be sealed for avoiding light and moisture.

Package：

25kgs craft bag with Carton box on pallet.

Please note: ***This technical index and recommending application information is based on the present knowledge for reference only. Necessary test is needed before you put into use. ***